TURBO-LINER PRIME-U ACCELERATOR
Primer Accelerator

MIXING
Turbo Liner Prime-U Accelerator may be mixed into all
Turbo Liner Prime-U®  surface primer coating by using a mechanical mixer. Mix Turbo Liner Prime-U Accelerator into the Turbo Liner Primer-U until a homogeneous mixture and color is obtained.

PACKAGING
1 quart (0.95 liter) can

COLOR
Clear (Pale Yellow)

FEATURES
™Fast Cure Time
™Saves in Labor Cost - Apply Two Coats in One Day

For use in Turbo Liner Prime-U only.

DESCRIPTION
Turbo Liner Prime-U Accelerator is a single component, low viscosity, accelerating agent. This accelerator enhances the moisture curing characteristics of Turbo Liner Prime-U.

Turbo Liner Prime-U Accelerator may react with atmospheric moisture
and render it unusable.

Do not dilute under any circumstance.

WARNING
This product contains Curatives.

This product is considered Dangerous Goods. DOT

regulations classify it as:

CORROSIVE  LIQUID

N.O.S.,

Volume Mixing Ratio:
.5 pint Prime-U Accelerator to 1 gallon Prime-U® (0.24 liters Prime-U Accelerator to 3.79 liters Prime-U)

(Contains Amine), Class 8, UN 1760, PG III.

-or-

1 Quart Prime-U Accelerator to 5 gallons Prime-U® (0.95 liters Prime-U Accelerator to 18.9 liters Prime-U®)

The pot life of the resulting compound is approximately 1-3
hours at 75°F (24°C) and 50% relative humidity.

EQUIPMENT CLEANUP
Equipment should be cleaned with an environmentally safe solvent, as permitted under local regulations, immediately after use.

STORAGE
Prime-U Accelerator has a shelf life of one (1) year from date of manufacture in original, factory-sealed containers.

LIMITATIONS
Not recommended for indoor applications.

Should be used in well-ventilated areas due to its strong
odor.

Containers that have been opened must be used within 1-3
hours.

Turbo Products, Inc. ♦ 1 West Cameron, Kellogg, ID 83837, USA ♦ Tel: 877-678-8726 ♦ www.turboliner.com

TECHNICAL DATA
Pot Life (during application) .............................. 1-3 hours
Volume Mixing Ratio,
Prime-U Accelerator : Turbo Liner Prime-U .... 1:20
Specific Gravity  ................................................. 0.87
Viscosity at 75°F (24°C)  ................................... 100 ± 50 cps

Please read all information in the general guidelines, product data sheets, guide specifications and material safety data sheets (MSDS) before applying material. Published technical data and instructions are subject to change without notice. Contact your local Turbo Products representative or visit our website for current technical data and instructions.
DISCLAIMER
All guidelines, recommendations, statements, and technical data contained herein are based on information and tests we believe to be reliable and correct, but accuracy and completeness of said tests are not guaranteed and are not to be construed as a warranty, either expressed or implied. It is the users responsibility to satisfy himself, by his own information and test, to determine suitability of the product for his own intended use, application and job situation and user assumes all risk and liability resulting from his use of the product. We do not suggest or guarantee that any hazard listed herein are the only ones which may exist. Neither seller nor manufacturer shall be liable to the buyer or any third person for any injury, loss or damage directly or indirectly resulting from use of, or inability to use, the product. Recommendations or statements, whether in writing or oral, other than those contained herein shall not be binding upon the manufacturer, unless in writing and signed by a corporate officer of the manufacturer. Technical and application information is provided for the purpose of establishing a general profile of the material and proper application procedures. Test performance results were obtained in a controlled environment and Turbo Products makes no claim that these tests or any other tests, accurately represent all environments.

Turbo Products, Inc. ♦ 1 West Cameron, Kellogg, ID 83837, USA ♦ Tel: 877-678-8726 ♦ www.turboliner.com ♦ Copyright© January 2011